## Slide 1: Chemistry & Materials with the ADF Modeling Suite
Fedor Goumans, goumans@scm.com
Seminar Yale, 1 December 2017

## Slide 2: Outline
Background
ADF: powerful molecular DFT
  Spectroscopy: NMR, EPR, VCD, UV, XAS
  Advanced solvation / environments
BAND: periodic DFT
  (2D) Materials
DFTB: fast approximate DFT
ReaxFF: Reactive MD
  Dynamics of large complicated systems
COSMO-RS: fluid thermodynamics
  VLE, LLE, logP, solubility
Integrated GUI – use out of the box
Scripting: workflows & automation

## Slide 3: Background
ADF = first DFT code for chemistry (1970s)
Baerends@VU (>’73), Ziegler@Calgary✝ (>’75)
SCM: Spin-off company 1995
15 people (10 senior PhD’s) + 5 EU fellows
Many academic collaborators / EU networks
  ~120 authors
  New functionality
SCM: development, debug, port, optimize,
docs & support
Papers with
“DFT and Chemistry”

## Slide 4
The SCM team
Olivier:
GUI
Alexei:
ADF
ReaxFF
Erik:
ADF
COSMO-RS
Pier:
BAND
Mirko:
ADF
BAND
Hans:
Linux
GPU
Python
Thomas:
DFTB
Scripting
Laurens:
GUI
Ole: Support
Scientist
Evert Jan:
Adviser
Fedor:
Marketing
Sergio:
Collaborations
Frieda:
Invoices
Licenses
Kitty:
Finance
Stan:
CEO
Michal:
python scripting
Robert:
DFTB
Nick:
COSMO-RS
Tomas:
ReaxFF
Anna:
ReaxFF

## Slide 5: Making computational chemistry work for you

## Slide 6: ADF: Molecular DFT
Strong & unique points
All-electron Slaters, all elements
Relativity: ZORA (SR, SOC)
Spectroscopy
  EPR, NMR, IR (VCD), UVVIS, XAS
Bonding analysis:
  Fragment-based approach
  ETS-NOCV, QTAIM, MO diagrams, NCI, ....
  Transfer integrals (charge mobility)
Environments
  Subsystem DFT (FDE), DIM/QM, QM/MM

## Slide 7: Hydrogen evolution catalyst characterized with EPR
W. Wang, M. J. Nilges, T. B. Rauchfuss, and M. Stein, Isolation of a Mixed Valence Diiron Hydride: Evidence for a Spectator Hydride in Hydrogen Evolution Catalysis J. Am. Chem. Soc. 135, 3633-3639 (2013)
Notes: In a quest to further advance the hydrogen economy, diiron complexes, mimicking [FeFe]-H2ases have been widely studied as cheaper and more sustainable catalysts for the hydrogen evolution reaction (HER). Researchers from the University of Illinois and the MPI for Dynamics of Complex Technical Systems have isolated and characterized a mixed-valence diiron hydride, giving unique insight in the mechanistic cycle for this class of bio-mimetic HER catalysts.
The calculated (ZORA-DFT) geometries, IR shifts, and EPR parameters are in good agreement agreement with the experimental findings and yield insight in the spin distribution in the unsymmetric and symmetric isomers.

## Slide 8
Accurate NMR: all-electron, STOs, and ZORA
L. A. Truflandier, E. Brendler, J. Wagler, J. Autschbach, 29Si DFT/NMR Observation of Spin-Orbit Effect in Metallasilatrane Sheds Some Light on the Strength of the Metal→Silicon Interaction Alkyl Complexes Angew. Chem. Int. Ed. 50, 255 (2011)
Heavy Atom effect on Light Atom (HALA)
  Even through Pt→Si dative bond
Spin-Orbit Coupling gets NMR coupling right
29Si

## Slide 9: Spin-orbit coupling increases dye efficiency
E. Ronca, F. de Angelis, and S. Fantacci, TDDFT Modeling of Spin-Orbit Coupling in Ru and Os Solar Cell Sensitizers, JPC C, 118, 17067-17078 (2014) see also: Impact of Spin–Orbit Coupling on Photocurrent Generation in Ruthenium Dye-Sensitized Solar Cells, JPCL, 5, 375-380 (2014)
SOC necessary for Os: increases NIR absorption
Less strong for Rh, but still improves IPCE through spectral broadening

## Slide 10: Phosphorescent OLED emitters
ADF tutorial online
K. Mori, T. P. M. Goumans, E. van Lenthe, F. Wang, PCCP 16, 14523 (2014)
Optimize OLED performance
  High charge mobility
  Fast ISC: S1→T1
  Phosphorescence T1→ S0
  Classically forbidden
  Need spin-orbit coupling
ADF features
  SOC-TDDFT: kphos
  SOCME: kISC
  Transfer integrals (mobilities)
  Vibrationally resolved abs/em
23 Ir, Rh, Ru, Os, Pt, Re complexes

## Slide 11: Intersystem crossing: spin-orbit coupling
Phys. Chem. Chem. Phys. 16, 26184-26192 (2014)
lexc-dependent quantum yield
SOCME negligible for S1-Tn
ISC from higher Sn states
El-Sayed for organometallics:
SOC is largest when:
both S (1dπ*) and T (3d’π*) are MLCT
different d-orbitals are involved (d ≠ d’).
Surface-Hopping Dynamics Ru(bpy)32+
Interface SHARC-ADF with ISC (SOC)
ISC from higher Sn states within 26 ± 3 fs
Atkins & Gonzalez
J. Phys. Chem. Lett.,, 8, 3840–3845 (2017)
Notes: The Os(fipz)(tfa)(CO)3 (tfa = trifluoroacetate, fipz=3-trifluoromethyl-5-(1-isoquinolinyl)-1,2-pyrazole) complex shows excitation-dependent emission quantum yield. The higher-energy excitation (< 340 nm) contributes more to phosphorescence than fluorescence, implying stronger intersystem crossing (ISC) for highly excited singlet states. Theoretical calculations confirm that the spin-orbit coupling (SOC) integrals between the lowest singlet excited state, S1, and the low-lying triplet excited states Tn (n=1-10), are negligibly small, whereas the higher singlet states show much stronger SOC with triplet excited states.

## Slide 12: Non-adiabatic dynamics: SHARC
M. Richter, P. Marquetand, J. González-Vázquez, I. Sola, L. González, SHARC – ab initio molecular dynamics with surface hopping in the adiabatic representation including arbitrary couplings, J. Chem. Theory Comput., 7, 1253-1258 (2011).
S. Mai, P. Marquetand, L. González, A General Method to Describe Intersystem Crossing in Trajectory Surface Hopping, Int. J. Quantum Chem., 115, 1215 (2015).
collaboration with Gonzalez, Oppel
Surface Hopping w/ ARbitrary Couplings
kISC through non-adiabatic couplings + SOC
to be extended to (TD)DFTB

## Slide 13: XANES/NEXAFS: Ru water-splitting cat.
I. Alperovich, G. Smolentsev, D. Moonshiram, J.W. Jurss, J.J. Concepcion, T.J. Meyer, A. Soldatov, Y. Pushkar Understanding the Electronic Structure of 4d Metal Complexes: From Molecular Spinors to L-Edge Spectra of a di-Ru Catalyst J. Am. Chem. Soc., 133 15786-15794 (2011).
SOC necessary for L2,3
  Selected (core) excitations
  FDMNES, FEFF fails
  New: LFDFT
K-edges, XPS
  Fast Slater-TS or TP
  KS energies or DSCF
  Polarization-resolved possible
  Helps determine exp. structure
  e.g. J. Phys. Chem. C 116, 18910 (2012); 141, 044313 (2014)
Notes: Ru L2,3-edge spectra well-reproduced by looking at transitions between spinors. 1-electron methods (FDMNES, FEFF) fail even for the simplest RuNH3 complex. Water splitting catalyst.
In the Transition State you move half an electron from initial to final orbital and take the SCF KS eigenvalue difference as excitation energy. This is the original Slater formulation and is justfied doing a Taylor expansion of total energy with respect to occupation numbers, it can be shown that errors arise from third order terms which are small. This however is not very practical: to converge SCF by putting half an electron in virtual orbitals is very hard,
usually it works only for the lowest virtuals. In order to avoid this problem one neglects the half an electron in virtual, this scheme (only half an electron
removed from occupied orbital) is called Transition Potential (TP) and is widely employed in XAS from K-edges.

## Slide 14: ETS-NOCV: bond & density decomposition
Molecule built from fragments
Bond analysis with meaningful terms:
Combine with NOCV (webinar)
  Orbital interactions / charge transfer
Also periodic 1D, 2D, 3D (tutorials)
  (Ad)sorption nanotbues, surfaces, MOFs etc.

## Slide 15: Catalyst design: activation strain model
Chem. Eur. J. (communication) 2009, 15, 6112
Org. Biomol. Chem. 2010, 8, 3118
Nature Chem. 2010, 2, 417
EDA along the reaction path
Bite-Angle Effect: Activation Strain analyses:
• HOMO–LUMO interaction marginally improved
• But: strain reduced by building it into catalyst
TS
Latest reviews:
Chem. Soc. Rev. 2014, 43, 4953
WIRES Comput. Mol. Sci. 2015, 5, 324

## Slide 16: Catalyst natural selection: survival of the weakest
Increased bite angle dppe → dppb
Improved electronic interaction and larger repulsive strain
Strain outweighs electronic interactions → dppb most destabilized → best catalyt
J. Wassenaar, et al. Catalyst selection based on intermediate stability measured by mass spectrometry. Nature Chem. 2, 417 (2010)
Notes: We introduce a new selection method that focuses on the stability of catalytic intermediates measured by mass spectrometry (ESI-MS), competition experiment. The stability of the intermediate relates inversely to the reactivity of the catalyst, which forms the basis of a catalyst-screening protocol in which less-abundant species represent the most-active catalysts, ‘the survival of the weakest’. We demonstrate this concept in the palladium-catalysed allylic alkylation reaction using diphosphine and IndolPhos ligands and support our results with high-level density functional theory calculations.
High-level DFT calculations show that destabilization of the intermediate Pd-allyl complexes is caused by steric repulsion between the ligand and the substrate for the diphosphine ligands, which overrules the counterbalancing electronic effect. Energy decomposition, strain energy

## Slide 17: Methods to calculate charge mobilities
Hopping transport:
  Charge transfer integrals (FO) - easy
  Electronic couplings from FDE
Band transport: effective mass tensors in BAND
Non-equilibrium Green’s Function (NEGF)
  transmission probabilities for single-molecule junctions
  quick calculation: wide-band limit
  also in BAND (periodic structures, fully self-consistent, bias) and in DFTB
h+

## Slide 18: Effective transfer integral Jeff = electronic coupling V
extract dimers
ADF tutorial online, ADF prints V / Jeff => use with Marcus theory for hopping rates
Anisotropic mobility:
S.-H. Wen et al., J. Phys. Chem. B 113, 8813 (2009)
Notes: 直行変換

## Slide 19: Beyond transfer integrals: environments with FDE
Pavanello & Neugebauer groups: Excitons: J. Chem. Phys. 138, 034104 (2013), charge separation: J. Chem. Phys. 140, 164103 (2014), charge transfer: J. Chem. Theory Comput. 2014, 10, 2546−2556
Frozen-Density Embedding
Subsystems: DFT-in-DFT
(or WFT-in-DFT)
Freeze-thaw
Linear scaling
Control over constraints
1993: Wesolowski & Warshel
ADF: Visscher, Neugebauer, Jacob, Pavanello
Couplings: electron transfer, exciton, charge separation, ....
Include environment / polarization at DFT level
Notes: With FDE you can take the diabatic states and work out the couplings from the diabatic Hamiltonian
This works for charge transfer, exciton coupling, polaron-exciton coupling

## Slide 20: Constrained Subsystem DFT: CSDFT
Ramos & Pavanello, Phys. Chem. Chem. Phys., 18, 21172 (2016)
localize charges and/or spins on a portion of a subsystem
Extended to excited states: XCDFT (in prep. - Pavanello)
Notes: Right: DNA hole transfer. A DNA trimer is split into two subsystems. On subsystem 1, the positive charge is localized on the PO4 group, or on the nucleobases. On subsystem 2, the diabat for hole transfer is the hole localized on the entire subsystem.

## Slide 21: BAND: Periodic DFT
bias = 0.1
bias = 0
Dielectric function ML ZnO
STM PtGe(100)
Band structure, pDOS, fat bands ZnO
Polarizing MoS2 with an eletric field

## Slide 22: BAND vs. Plane Wave codes
Atom centered basis functions, STO or NAO
  Compare cluster with periodic
  No pseudopotentials, all elements
  Core spectroscopy (core holes)
  Easy (orbital, density) analysis with GUI
  Fast for empty (1D, 2D, porous)
  xc: SCAN, MN15-L, HSE06, GLLB-sc, D3(BJ), ...
  Self-consistent NEGF
    Gate & bias potential
    Spin transport
True 2D surfaces, 1D polymers
  Het. catalysis: polarization, COSMO
  2D electronics (homogeneous E field)
  Nanotubes
Integrated Graphical Interface:
  Easy set up & analysis
  Switch: ADF, BAND & Quantum Espresso
crystal orbitals, periodic energy decomposition analysis
M. Raupach and M. Tonner, J. Chem. Phys. 142, 194105 (2015)

## Slide 23: Relativity makes your car start
R. Ahuja, A. Blomqvist, P. Larsson, P. Pyykkö, and P. Zaleski-Ejgierd, Phys. Rev. Lett. 106, 018301 (2011)
- Total and partial density of states (DOS) of lead in Lead (IV) oxide
- Strong relativistic shift in
both occupied and unoccupied Pb 6s states.
- Without relativity, 12V battery would be 2.4V!
Orange = lead 6s states, Green = lead 6p states.
NR = nonrelativistic, SR = scalar relativistic, SOC = self-consistent spin orbit coupling
SOC

## Slide 24
Dissociation at TMO – NP interface preferred
Aluminum acts as electron donor
Need 2D to polarize surface
Li, Croiset, Ricardez-Sandoval, J. Phys. Chem. C 2013, 117, 16907
CH4 and H2 dissociation on Ni/γ-Al2O3
Notes: 24

## Slide 25
3 eV/Å
Electron transport in MoWSeS monolayers in the presence of an external electric field, Phys. Chem. Chem. Phys. (2014)
Closing the band gap in 2D MoWSeS
Need 2D + homogeneous field
Plane wave: 3D + saw-tooth gives wrong behavior
Notes: 25

## Slide 26: Stretching-induced conductance: spin transport
Stretch: Fe LS => HS
Riccardo Frisenda, et. al. Stretching-Induced Conductance Increase in a Spin-Crossover Molecule. Nano letters 2016, 16(8), pp 4733-4737
spin-polarized BAND/NEGF calcs.: increased HS conductance
- Agrees with exp.

## Slide 27: DFTB: approximate DFT
Approximations (to DFT)
Nearest neighbors
Minimal basis
Elec & rep. parameters
Capabilities & Features
Much faster than DFT
  Molecules and periodic
Repulsive
  Geometries
  Vibrationally resolved excitations
  IR, phonons, MD
Electronic
  Band structures, MOs
  UV/VIS
  Electron transport (NEGF)
Pre-optimize or pre-screen
  Script or chain jobs
QN 2015: rep
QN 2013: ele
Band structures in Si crystals with PBE/TZP, matsci-0-3, QuaSiNaNo 2013

## Slide 28
2D PdS2 is
semiconducting as ML
semimetallic as BL
M.Ghorbani-Asl, A. Kuc, P. Miró, and T. Heine, A Single-Material Logical Junction Based on 2D Crystal PdS2, Adv. Mater. (2016)
DFTB-NEGF
channel lengths of about 2.5 nm
I–V characteristics tunable by gate voltage
Single 2D semiconductor material diode

## Slide 29: Fast excited states: TDDFTB
Removing 30% excitations reduces CPU time by 98% at no accuracy loss
Rüger, R., et al. , J. Chem. Theory Comput. 11, 157−167 (2015)
Notes: Ubiquitin: 1400 atoms

## Slide 30: Fast excited states: TDDFTB
Excited states gradients: FCF / vibronic states
S1 (v)→S0 (v’)
Rüger, R., et al. , J. Chem. Theory Comput. 11, 157−167 (2015)
J. Chem. Phys. 144, 184103 (2016)
DFT
DFTB
In ADF a TD approach is available with similar TB approximation, using DFT orbitals
Also available: Grimme’s sTDA & sTDDFT
11000 s
600 + 60s
10s
Rüger, R., et al. J. Chem. Phys. 145, 184102 (2016)
Notes: Fast approximations: besides TD-DFTB you can also use the TB approximation for the excitations with the DFT orbitals, which gives access to better (higher) excitations. Limiting step here are the DFT orbitals. TDDFTB can also calculate frequencies => vibrationally resolved spectra.

## Slide 31: Vibrationally resolved UV/VIS with TDDFTB
Adiabatic Hessian Franck-Condon, using (TD)DFTB gradients
Rüger, R., et al. J. Chem. Phys. 145, 184102 (2016)
Notes: Vibrationally resolved S0→ S1 absorption spectrum of pentarylene.
The arrows mark the vertical excitation energies. DFT/BH-LYP results from
Ref. 18. Experimental spectrum from Ref. 43.

## Slide 32: Propylene Oxide Hydrolysis over ZSM‑5 Zeolite
J. Phys. Chem. C 2014, 118, 21952−21962
Multi-layer DFT/DFTB3 calculations:
monoproplyene glycol formation preferred

## Slide 33: ReaxFF – reactive molecular dynamics
Pd-catalysed CO oxidation GCMC+ReaxFF
J. Chem. Phys., 139 044109 (2013)
Hydrogen embrittlement of steels
Phys. Chem. Chem. Phys. 18 761-771 (2016)
Li battery discharge: J. Electrochem. Soc.
161, E3009 (2014); PCCP, 17, 3383 (2015)
Crystallization TiO2 nano-particles in water Nano Lett. 14, 1836-1842 (2014)

## Slide 34: ReaxFF: introduction
Simulate complex systems at realistic scales
  Atomistic potentials: bond orders + charge update
A.C.T. van Duin et al ,J. Phys. Chem. A 2001 , 105, 9396-9409.

## Slide 35
No discontinuities in energy or forces
No pre-defined reaction sites or types
Only 1 atom type per element
General ReaxFF rules
Notes: User should not have to pre-define reactive sites or reaction pathways; potential functions should be able to automatically handle coordination changes associated with reactions.
force field should be able to determine equilibrium bond lengths, valence angles etc. from chemical environment.

## Slide 36
ReaxFF parameters, transferability
many elements studied
each pair needs bonded terms
validate force field
    GUI checks
    training data crucial
    application specific
New parameters
  ADF 2013: 17 sets, 19 elements
  ADF 2014: 38 sets, 29 elements
  ADF 2016: 58 sets, 38 elements
  ADF 2017: 79 sets, 38 elements
  van Duin, Goddard, others
  RxFF consulting
  MCFF optimizer

## Slide 37
ReaxFF tools in ADF Modeling Suite
GCMC: speed up thermo
fbMC: speed up kinetics
ChemTraYzer: Automated rates & pathways
Molecule gun: depositing molecules on surfaces
MCFF: parameterize ReaxFF force field

## Slide 38
Analyzing trajectories: events
M. Döntgen et al., J. Chem. Theory Comp. 11, 2517–2514 (2015)

## Slide 39
Dealing with the atomistic insight
ChemTraYzer: complete reaction network, rate constants, timeline, ..
M. Döntgen et al., J. Chem. Theory Comp. 11, 2517–2514 (2015)

## Slide 40
ChemTraYzer
M. Döntgen et al., J. Chem. Theory Comp. 11, 2517–2514 (2015)
Follow connectivity (BO in ReaxFF)
Tabulate changing species
  Identify identical species (SMILES, InChI)
  Reaction pathway: graph
Calculate fluxes, rate constants
Visualize network
  Interactively
  2D => 3D
  Follow reaction pathway

## Slide 41
Carbon nanotube formation: accelerate MD
ReaxFF acceleration:
fbMC tutorial
Neyts et al., J. Am. Chem. Soc. 133, 17225 (2011)
ReaxFF-MD + fbMC: healing of defects during sliding of network (steps 4-5).
First simulation showing growth of an armchair SWNT with definite chirality on catalyst.
pentagon formation
graphitic patches
cap development
carbon network slides over catalyst
part of metal gets freed
end of sliding,
chirality obtained
Molecule gun + fbMC video

## Slide 42
GCMC: What is stable (p,T)?
ReaxFF: What is active?
Grand Canonical Monte Carlo + ReaxFF
T.P. Senftle, R.J. Meyer, M.J. Janik, A.C.T. van Duin, J. Chem. Phys., 139 (2013) 044109
Reactive MD under actual conditions
ReaxFF +GCMC tutorial

## Slide 43: Discharge process Li-S batteries
M. M. Islam, A. Ostadhossein, O. Borodin, A. T. Yeates, W. W. Tipton, R. G. Hennig, N. Kumar, and A. C. T. van Duin, ReaxFF molecular dynamics simulations on lithiated sulfur cathode materials, Phys. Chem. Chem. Phys. 17, 3383-3393 (2015)
Voltage (V)
Cathode expands upon lithiation
  Captured by ReaxFF
Voltage during discharge (GCMC)
Diffusion induced stress

## Slide 44
Optimizing ReaxFF parameters
Highly complex global optimization:
  many parameters
  interdependent
  non-linear
  not always physically interpretable
E. Iype, et al., Parameterization of a Reactive Force Field Using a Monte Carlo Algorithm, J. Comp. Chem. 34, 1143-1154 (2013)

## Slide 45
Monte Carlo with Simulated Annealing
J. Comp. Chem. 34, 1143-1154 (2013)
xi,TS = reference
xi,ReaxFF = current ReaxFF
σi = weight
References include:
● Atomic charges
● Heat of formation
● Geometries (Bond/Angle/Dihedrals)
● Cell parameters
● Energies
Iteration

## Slide 46
Tying it all together: python
Links all modules + various tools
→ workflows & screening
→ (custom) post-processing
→ rapid prototyping
MOPAC

## Slide 47
Automating ReaxFF parameterization
ADF
BAND
training set
ReaxFF
MCFF
reaction network
ChemTraYzer
new species?
Ultimately:
(more) GUI support
Production runs
+
Analysis

## Slide 48
NEW: eReaxFF- include Explicit Electrons/Holes
M. M. Islam, G. Kolesov, T. Verstraelen, E. Kaxiras, A. C. T. van Duin, J. Chem. Theory Comput 2016, 12 (8), 3463-3472.
e-
Electron transfer in a C12H19 radical
Time-scale needed for electron transfer from polyacetylene to the radical site at different T
Basic idea:
Electrons/Holes → additional particle
Electrons → Gaussian wave functions
ψ ∝ exp(−α(r−r′)2)
Enuc-elec depends on
    - nuclear charge
    - Gaussian exponent α
    - distance (nucleus – electron)
Further dependencies/coupling terms
    - atom type, bond type, coordination
    - electron – electron
#electrons per nucleus can be fractional → 'split electron'
Atom
+ e-
#Val. electrons: up
Valency : down
Atom
+ h
#Val. electrons: down Valency : up
First proof of concept results:

## Slide 49
eReaxFF – Solid-Electrolyte Interfaces
M. M. Islam and A. C. T. van Duin, J. Phys. Chem. C 2016, 120 (48), 27128-27134.
Reductive decomposition of ethylene carbonate in Li ion batteries
eReaxFF video

## Slide 50
From quantum chemistry to chemical engineering thermodynamics
COSMO-RS: fluid properties

## Slide 51
  s-profile: charge density on COSMO (e=∞) surface
  pair-wise interaction between molecules
  electrostatic interactions + hydrogen bond
  pseudo-chemical potentials
  random mixture approximation, equilibrium
  statistical thermodynamics
From QM to statistical thermodynamics
  chemical potential => activity coefficients => properties

## Slide 52
(acid) AH (aq) + H2O (l) → H3O+ (aq) + A- (aq)
(base) BH+ (aq) + H2O (l) → H3O+ (aq) + B (aq)
Empirical fitting ΔGdiss against experimental pKa
(acid) pKa = 0.62 ΔGdiss/(RT ln(10)) + 2.10
(base) pKa = 0.67 ΔGdiss/(RT ln(10)) - 2.00
See COSMO-RS tutorials and work by Michelle Coote & Junming Ho
pKa values: fitting ΔGdiss
Notes: pKa = -log Ka
Ka=lA-][H+]/[AH]
pH = pKa + log[A-]/[HA]

## Slide 53
log PA/B = log {[solute]A/[solute]B}
Experimental values taken from: A. Klamt et al., J. Phys. Chem. A 102 (1998) 5074
Partition coefficients (logP)
Notes: The log of the solute concentration in solventa A divided by the solute concentration in solvent B
Thus the relative solubility

## Slide 54
Z. Lei, C. Dai, and B. Chen, Gas Solubility in Ionic Liquids, Chem. Rev., 114, 1289−1326 (2014).
Prediction beyond parametrization (opposed to UNIFAC)
Works well for SO2 solubilities
Improvements needed for CO2
COSMO-RS VLE: solubility in ionic liquids
Notes: COSMO-RS prediction of SO2 solubilities (solid lines) in [BMIM]+[MeSO4]−, compared with experiments (symbols) at different temperatures (283, 298.1, 323.1, 348.1 K)

## Slide 55: 1 GUI: build, run & analyze

## Slide 56: Summary
Molecular DFT with ADF
  Unique features for organic electronics
  Fast + accurate TDDFT - nanoparticle optical properties
BAND AO-based
  Optical and electronic properties of 2D systems
  Easy orbital & density analysis
  NEGF: Charge and spin transport
DFTB: faster more approximate
  Spectroscopy, reactivity, dynamics
  NEGF: transmission, charge transport
ReaxFF: reactive MD large, complex systems
  Monte Carlo methods to speed up time / equilibrium
  New: eReaxFF for batteries / Redox reactions
Synergy between all modules + GUI

## Slide 57
Recent pNMR paper: Direct Detection of 17O in Gd(DOTA)] by NMR Spectroscopy, Chem. Eur. J. 21, 1955-1960 (2015)

## Slide 58: CV-DFT works for charge-separated states
M. Krykunov, S. Grimme, T. Ziegler,
J. Chem. Theory Comput. 8 (2012) 4434.
TDDFT FAILS
Constricted-variational DFT
  Delta-SCF like approach on TDDFT
  Constraint: 1e in total removed from occupied
  Alternative to TDDFT/RSH: use with GGAs

## Slide 59: Fast excited state calculations
R. Rüger, et al. http://arxiv.org/abs/1603.02571
11000 s
600 + 60s
10s
Also available: sTDDFT, sTDA
TDDFTB on DFT orbitals: TD-DFT+TB

## Slide 60: Efficient TDDFT for nanoparticle plasmons
O. Baseggio, M. De Vetta, G. Fronzoni, M. Stener, L. Sementa, A. Fortunelli, and A. Calzolari, J. Phys. Chem. C 120, 12773 (2016).

## Slide 61: Optical Properties of Silver and Gold Nanoparticles
J. Am. Chem. Soc., 136, 14933-14940 (2014) J. Phys. Chem. C, 118, 12450-12458 (2014)
Relativistic TDDFT (ZORA), Symmetry, SAOP, Slater-type Orbitals
Aikens, Khanna, Schatz, Stener, …

## Slide 62: Faster TDDFT: complex polarizability (aux. basis)
Removes Davidson diagonalization bottleneck
  Large systems (>1000 Au/Ag) & higher excitation energies
Analyze plasmons: TCM, scaling factor, induced r
CD rotational strengths ‘free’
Coming soon – not yet documented
New complex polarizability algorithm
Baseggio, Fronzoni, Stener, J Chem Phys. 143, 024106

## Slide 63: Coupled TDDFT – atomistic electrodynamics (DIM/QM)
Plasmon-exciton hybridization
  enhanced molecular absorption
Surface-enhanced Raman scattering
  including optically active (SEROA)
Plasmon enhanced photochemistry
New: NLO: SEHRS & more
TDDFT + potential atomistic electrodynamics
DRF (polarizable force field)
Fit capacitance & polarizability to bulk (BAND)
developed by Lasse Jensen group,
see also his web presentation.
Review: Acc. Chem. Res. 47, 88–99 (2014)

## Slide 64: New methods for NLO (Jensen et al.)
Damped quadratic response theory + DIM: SEHRS
Hu, Z.; Chulhai, V. D.; Jensen, L. J. Chem. Theor. Comput., 2016
Notes: Crystal Violet damped quadratic response theory, as opposed to SOS (where a few states dominate), SER

## Slide 65: Damped cubic response (gamma): TPA, THG
Two Photon Absorption:
Third Harmonic Generation:
Hu, Z; Autschbach, J.; Jensen, L. J. Chem. Theor. Comput., 2016, 12, 1295
Other γ properties
OKE
EFIOR
EFISHG
NLR
2HRS

## Slide 66
Spin states: Slaters vs Gaussians
J. Phys. Chem. A, 112 (28), p. 6384, 2008, Güell, Luis, Sola, and Swart
“Slaters give consistent and rapidly converging results outperforming Gaussians and ECP”
  STOs converge rapidly, GTOs slowly
  ECPs give systematically different results
  sGTOs give correct results
  (JPCA 2010, 114, 7191)
Notes: 66
J. Phys. Chem. A, 112 (28), p. 6384, 2008, Güell, Luis, Sola, and Swart, compare ADF's Slater Type Orbital (STO) basis sets to Gaussian Type Orbitals (GTO) basis sets in a systematic study on spin-state energies of iron complexes. Their findings are summarized in the graph below.
Slow convergence with Gaussian basis sets
The abstract states that "STO basis sets give consistent and rapidly converging results, while the convergence with respect to basis set size is much slower for the GTO basis sets." They conjecture that this may be related to "the cusps at the nuclei (correctly described in STO, incorrectly described in GTO)". The GTO basis sets of standard size in particular have problems with the high-spin state.
No convergence with ECP basis sets
In case GTO basis sets are combined with Effective Core Potentials (ECPs), the results worsen in the sense that the common basis set limit for STO's and GTO's does not seem to be reached even for quite large ECP basis sets.

## Slide 67
Broken-Symmetry DFT: multi-nuclear complexes (CcO, [4Fe4S], …)
Environment: COSMO and SCRF (favors higher charged states)
Antibiotics/antimalarial drugs with new mode of action: inhibit MEP (DOXP) pathway
P. Blachly, … Bashford & Noodleman, Use of Broken-Symmetry Density Functional Theory To Characterize the IspH Oxidized State: Implications for IspH Mechanism and Inhibition, J. Chem. Theory Comput. 2014, 10, 3871 (2014)
Notes: 67
isoprenoid biosynthesis pathway in humans/animals follows different route: DMAPP and IPP through a mevalonate-dependent pathway that is distinct from the MEP pathway
Approval of fosmidomycin, an antimalarial drug that targets 1-deoxy-D-xylulose 5-
phosphate reductoisomerase (DOXP reductase, also referred to as Dxr or IspC), the second enzyme in the MEP
pathway.18−20

## Slide 68: Charge generation in fullerene-based OPVs
J. Am. Chem. Soc., 136, 2876−2884 (2014)
Charge generation facilitated by resonant coupling of singlet excitons in polymer donors to fullerene electronic states
Diagonal couplings
Off-diagonal couplings
(transfer integrals)

## Slide 69: Singlet Fission Yields in Organic Crystals
N. Renaud, P. A. Sherratt, and M. A. Ratner, Mapping the Relation between Stacking Geometries and Singlet Fission Yield in a Class of Organic Crystals, J. Phys. Chem. Lett., 4, 1065-1069 (2013)
Direct pathway dominates SF
Yields up to 132% possible, depends on crystal packing

## Slide 70: eXcited Constrained DFT (XCDFT), in prep
Pavanello research group, under development
XCDFT localizes excitations: Good alternative to △SCF and TDDFT

## Slide 71: Thermally Activated Delayed Fluorescence
Optimize radiative rate
Minimize S1-T1 gap
Maximize SOC
Maximize kphos & kTADF
Z.-M. su et al. Dyes & Pigments 2017,
Bredas et al. J. Am. Chem. Soc. 2017, 139, 4042−4051
ADF tutorial in progress

## Slide 72: Vibronic fine structure T1 → S0 OLED phosphor Pt complex
Excellent agreement vibrational progression FCF T1-S0
0-0 well reproduced by Delta SCF calculation (22,000 cm-1)
ADF tutorial online

## Slide 73: Energy decomposition analysis
∆E = ∆Eprep + ∆Eint
∆Velstat + ∆EPauli + ∆Eoi + ∆Edisp
∆Esteric = ∆Velstat + ∆Epauli
∆Eoi = decomposed in irreps.
∆Eprep = geometry ’deformation’ energy
Chem. Soc. Rev. 2014, 43, 4953;
WIRES Comput. Mol. Sci. 2015, 5, 324
Oline tutorial & teaching materials
fragments => molecule
Notes: The term ΔVelstat corresponds to the classical electrostatic interaction between the unperturbed charge distributions of the prepared (i.e. deformed) fragments and is usually attractive. The Pauli repulsion ΔEPauli comprises the destabilizing interactions between occupied orbitals and is responsible for any steric repulsion. The orbital interaction ΔEoi in any MO model, and therefore also in Kohn-Sham theory, accounts for charge transfer (i.e., donor-acceptor interactions between occupied orbitals on NH3 with unoccupied orbitals of BH3, including the HOMO-LUMO interactions) and polarization (empty/occupied orbital mixing on one fragment due to the presence of another fragment).

## Slide 74: DFT-D3 XC functionals in ADF & BAND
S.Grimme, J. Antony, S. Ehrlich, and H. Krieg: J. Chem. Phys. 132, 154104 (2010).
- Less empirical than earlier DFT-D2
Asymptotically correct
Available for elements Z = 1-9`4
Dispersion coefficients and cutoff radii computed explicitly
Dispersion coefficients independent of connectivity
- Similar or better accuracy for light elements, better for heavy ones
Notes: Grimme and his coworkers at the Universität Münster outlined the parameterization of this new correction, dubbed DFT-D3, in a recent issue of The Journal of Chemical Physics 132, 154104 (2010). Here they list the advantages of the new method as the following:
It is less empirical, i.e., the most important parameters are computed from first principles by standard Kohn-Sham (KS)-(TD)DFT. The approach is asymptotically correct with all DFs for finite systems (molecules) or nonmetallic infinite systems. It gives the almost exact dispersion energy for a gas of weakly interacting neutral atoms and smoothly interpolates to molecular (bulk) regions. It provides a consistent description of all chemically relevant elements of the periodic system (nuclear charge Z = 1-94). Atom pair-specific dispersion coefficients and cutoff radii are explicitly computed. Coordination number (geometry) dependent dispersion coefficients are used that do not rely on atom connectivity information (differentiable energy expression). It provides similar or better accuracy for "light" molecules and a strongly improved description of metallic and "heavier" systems.
Above: The adsorption energy of perylene-tetracarboxylic-dianhydride (PTCDA) on a gold (111) surface as a function of distance. Results without (PBE) and with dispersion corrections (PBE-D2, PBE-D3) are shown. The experimental distance is 3.27Å. The vdW-DF result is from PCCP, 12, 4759 (2010).
The article continues by, among other things, demonstrating how this new DFT-D version decreases the mean absolute deviations for a benchmark set of non-covalent interactions by 15-40% over the previous version. Professor Grimme notes that the more significant errors in dispersion energy can be expected for modeling highly charged systems. See section III-F of the original paper for more details.
DFT-D3 is now available in the development snapshots of ADF and BAND, versions r23091 and later. They can be downloaded at http://www.scm.com/SCMForms/DownloadSnapshots.jsp. Instructions on the use of this functional can be found in the ADF developer's change-log at http://www.scm.com/Downloads/ChangeLog-trunk.html.

## Slide 75
A. Berger, Fully parameter-free calculation of optical spectra for insulators, semiconductors and metals from a simple polarization functional, Phys. Rev. Lett. 115, 137402 (2015)
TDCDFT/RPA + GW scissors + a
Accounts for bound excitons & Drude tails
Parameter-free polarization functional
e2(w)
Notes: The main failures of standard approximations such as the random-phase approximation (RPA) and the adiabatic local-density approximation (ALDA) [9] are: 1) the underestimation of the onset of the absorption; 2) the underestimation of the intensity of continuum excitons; 3) the absence of bound excitons; 4) the absence of Drude tails in the spectra of metals.
Solution:
We calculate the macroscopic dielectric function using an efficient TDCDFT approach [26, 27] within the RPA (including a scissors shift obtained from GW); 2) We apply a simple dynamical polarization functional (see Eq. (14) below) that accounts for continuum and bound excitons as well as Drude tails.
macroscopic dielectric tensor ǫ ↔ M (ω) can be obtained from the electric susceptibility according to ǫ ↔ M (ω) = 1 + 4πχ ↔ e(ω).
75

## Slide 76
Fixing the band gap ‘problem’
Kohn-Sham gap ≠ fundamental gap
DFT underestimates band gap
  underlying problem: integer derivative discontinuity in vxc
  Egap = I – A + Δxc
Possible ‘solutions’
  many-body perturbation (GW) (not yet available in BAND)
  (screened) hybrids, e.g. HSE06
  LDA/GGA + U (localize d, f electrons in TMO)
  TB-mBJ (fitted to band gaps)
  GLLB-sc (includes explicit Δxc)
Notes: 76

## Slide 77
Accurate Band Gaps of Semiconductors and Insulators with a Semilocal Exchange-Correlation Potential Phys. Rev. Lett. 102, 226401 (2009).
Tran & Blaha’s modified Becke-Johnson (TB-mBJ)
Parameterized for inorganic semiconductors
Has adjustable parameters
  E.g. for hybrid perovskites
Includes volume term => 3D only
  ‘trick’ for 2D possible
Notes: revTPSS META-GGA: A WORKHORSE SEMILOCAL DENSITY FUNCTIONAL FOR CONDENSED MATTER PHYSICS AND QUANTUM CHEMISTRY
Mean absolute error (in kcal/mol) for the atomization energies of the representative AE6 molecules.
Mean absolute error (in Angstrom) for the lattice constants of 21 solids, computed with BAND.
Standard density functionals are biased toward the accurate description of either atoms and molecules (PBE GGA, TPSS meta-GGA) or solids (AM05 GGA, PBEsol GGA). But the nonempirical revTPSS meta-GGA achieves unbiased accuracy for atoms, molecules, solids, and solid surfaces (and hopefully for chemistry on surfaces).
New: HTBS: 7.1 for AE6, similar lattice as PBE
77

## Slide 78
GLLB-sc can also be applied to 2D, 1D
GLLB-SC: good band gaps for good reason?
Kohn-Sham potential with discontinuity for band gap materials M. Kuisma, et al. Phys. Rev. B 82, 115106 (2010)
Notes: Kohn-Sham band gap three leftmost, green and the discontinuity on top contribution to the quasiparticle total gap from our LDA, GLLB exchange only, and GLLB-S Ccalculations. The True DFT KS gaps rightmost, yellow with the discontinuity from GW top, red are shown for comparison.
78

## Slide 79
PBE 1.898
GLLB-sc 3.201 (Δxc = 0.92)
TB-mBJ 3.296
Non-relativistic:
TB-mBJ/NR 3.494
GLLB-sc/NR 3.487
Smaller basis:
GLLB-sc/TZP 3.253
Exp: 3.2 eV
(SR-TZ2P-AE, k=5 (75 k-points), acc=5)
Experimental gap
Fixing GaN band gap
Notes: 79

## Slide 80: Density-functional Based Tight-Binding (DFTB)

## Slide 81
How to accelerate dynamics?
Temperature - dynamics OK?
Metadynamics - collective variables
Parallel replica dynamics
Monte Carlo
  Grand-canonical: thermodynamics
  force bias – associated time scale?
Bond boost
…...
J. Chem. Phys., 139 (2013) 044109
J.Am. Chem. Soc. 134,
1256–1260 (2012)

## Slide 82: Teflon protects electrolyte in Li battery
M. M. Islam, V. S. Bryantsev, and A. C. T. van Duin, ReaxFF Reactive Force Field Simulations on the Influence of Teflon on Electrolyte Decomposition during Li/SWCNT Anode Discharge in Lithium-Sulfur Batteries, J. Electrochem. Soc. 161, E3009-E3014 (2014).
Teflon coating acts as buffer for Li-S batteries, reducing thermal electrolyte decomposition
Temperature profiles at 10ps after discharge from Li-SWCNT electrode (blue 60 K, red >1000 K)
Teflon
High T gradient:
1130 K
60 K

## Slide 83: Teflon protects electrolyte in Li battery
Teflon layer on anode-electrolyte interface significantly reduces lithium reactivity and diffusion through the electrolyte phase
J. Electrochem. Soc. 161, E3009-E3014 (2014).

## Slide 84
R. Xiong, S. I. Sandler, and R. I. Burnett, An Improvement to COSMO-SAC for Predicting Thermodynamic Properties, Ind. Eng. Chem. Res., 53, 8265–8278 (2014).
Includes dispersive mixture interaction:
Reduces logP errors by 10% vs 2010 (992 OW, 829 water-others)
Also improved VLE predictions
COSMO-SAC ADF-2013

## Slide 85
water/acetone (373K)
hexane/ethyl acetate (333.15K)
COSMO-SAC ADF-2013: improved VLE
R. Xiong, S. I. Sandler, and R. I. Burnett, An Improvement to COSMO-SAC for Predicting Thermodynamic Properties, Ind. Eng. Chem. Res., 53, 8265–8278 (2014).